## Slide 1: Engineering center «High-temperature composite materials"
created by association with JSC «Kompozit» - materials science leading enterprise of the State Corporation «Roscosmos»
Korolyov, 1 Stadionnaya street
www.kompozit-ut.ru
LEONOV Moscow Region
University of Technology

## Slide 2
www.kompozit-ut.ru
Temperature, °С
20
200
Density, g/см3
1000
1500
various steel grades
titanium
aluminium
*
*
New formulations of polymeric composite material
Composite materials with carbon and ceramic matrixes
High-temperature composite materials
- traditional carbon and glass fiber plastics
High-temperature composite materials

## Slide 3
Laboratory of Automated Equipment
Children's Technopark "Quantorium"
Laboratory of heterogeneous synthesis of refractory materials
Head of laboratory
Candidate of Engineering Sciences I.A. Timofeev
Laboratory of CAD/CAM/CAE systems
Laboratory of new ways of forming reinforcing frame for composite materials
Head of laboratory Doctor of Sciences
A.V. Chesnokov
Basic department “Quality management and research in the field of new materials and technologies”
Head of the Department Doctor of Sciences
A.N. Timofeev
Engineering center «High-temperature composite materials»

## Slide 4
BN B4C HfC SiC
2015
2016
2017
2018
2019
2020
BNCVD
HfCCVD
SiCCVD
BNCVI
HfCCVI
B4CCVI, SiBCVI
BCl3+NH3 → BN + 3HCL
HfCl4+CH4 →HfC+4HCl
CH3SiCl3+CH4 →SiC+4HCl
2015
2016
2017
2018
2019
2020
Development of technology of chemical deposition from the gas phase by University

## Slide 5
Пластины ПНБ размером 80х120х3 мм
BCl3+NH3 → BN + 3HCL
ТУ 2155-1-16986658-2015
CVD technology of obtaining pyrolytic BN for the electronics industry
Appearance of products
The flow reactor isothermal dimensions of the working area
D100 mm H300 mm
Option | Result
Crystal lattice | hexagonal
Density, g/cub.sm. | 1,97-1,99
Fraction of impurities, % at. | 0,01

## Slide 6: Working dimension f300, h500. Maximum temperature 1300 C. Automated emission cleaning system. Powered by MTS, argon, hydrogen
High-temperature gas-vacuum furnace for deposition of silicon carbide from the gas phase of methyltrichlorosilane (MTS)

## Slide 7: CVD technology of obtaining pyrolytic HfC
HfCl4+CH4 →HfC+4HCl
The size of the chemical reactor D80 H 350 mm.
Continuous monitoring of the mass of HfCl4 in the process of evaporation.
Notes: Второе направление развиваемое на сегодняшний день в МГОТУ это CVD технология получения карбида гафния из тетрахлорида гафния и метана

## Slide 8: Braiding machine РП64-1-130
kompozit-ut.ru
Braiding technologies
Contour weaving by Russian carbon high-strength and high-modulus yarns .
Contouring weaving on two and three axial (with skeletal reinforcement) schemes.
Contouring weaving products with a straight and curved axis.
Contouring weaving products with a closed axis .
Application of an interlayer layer with a continuous surface hiding power up to 200 mm in diameter.
Application of an interlayer layer to larger diameters with the formation of a network structure.
Contour weaving of products of unlimited length.
KUKA robot

## Slide 9
www.kompozit-ut.ru
Braiding technologies
Technology for the production of complex profile composite preforms
Possible cross-section of the frames:
Taleplerine frames
Possible type of preforms

## Slide 10
The software allows:
to obtain a three-dimensional model of interlacing of bundles for analysis of the obtained structure and modeling of the strength characteristics of the product;
on the basis of the product model, develop control programs for the braiding machine with the required requirements for the method of laying the bundle-a constant reinforcement angle or a constant surface density of the bundles.
kompozit-ut.ru
Software for modeling and controlling the process of braiding

## Slide 11
kompozit-ut.ru
preform samples
Preform modeling software developed
Automated installation of diagonal weaving 5x5

## Slide 12
A truss structure for the installation of electrical wiring in spacecraft was made
Braid-pultrusion technology for obtaining profiles, stringers, frames and other elements of truss structures

## Slide 13
High temperature carbon fiber on the basis of polyetheretherketone
Continuosly carbon reinforced PEEK have the similar (not lower) properties like regular plastics with thermoreactive matrix.
Carbon fiber reinforced PEEK on the strength of 1.5-4 times greater than aluminum alloys, and 2-3 times higher than engineering plastics at temperatures over 200°C .
A price comparable to aluminum parts at mass production.
Density reinforced PEEK 2 times lower aluminum.
Temperature operation completely replaces the aluminum.
Fasteners and sheet prefabricated from reinforced Peace
polyetheretherketone
CARBON FIBER
Milled fiber – injection molding.Thread, harness – winding, weaving, braiding.Ribbon, fabric – layout.
High temperature (Process Temperature up to 350°С) carbonplastic
kompozit-ut.ru

## Slide 14
kompozit-ut.ru
Modernized extruder with a spinneret for the production of multifilament yarn from PEEK
PEEK multifilament yarn
Manufacturing technology of PEEK multifilament yarn

## Slide 15
Technology of combining carbon and PEEK yarn
Braided Preform Technology
Technology of thermopressing preforms with a thermoplastic matrix
Products based on continuously reinforced thermoplastics

## Slide 16
CVD BN for the electronics industry
CVD SiC for electronic industry
3. Siliconized details including
4. Thermoplastic Polymers fittings, includes PEEK fittings
5. Production of preforms of various types, for thermoplastic materials, for high-temperature products and for radio-transparent products.
Possible areas for cooperation